Technical Data Sheet                                     ISSUE 2

Bio-Ropelube 00                                                  (Product Code: PC 1195)

Product Description

BIO-ROPELUBE 00 is highly water and hydrocarbon resistant biodegradable semi-fluid, solvent free wire rope lubricant designed to meet the lubrication and corrosion prevention requirements of wire ropes working under all conditions. Typical application areas are dockside cranes, draglines, water treatment and situations where a biodegradable lubricant is preferred for environmental reasons.

The ingredients used in the manufacture of BIO-ROPELUBE 00 naturally biodegrade by micro-organisms, so making this product environmentally friendly when compared to conventional rope lubricants.

Outstanding Features

- Biodegradable – environmentally acceptable

- Provides excellent internal and external protection, extending rope service life

- Addition of molybdenum disulphide, reduces wear between the strands of the rope

- Water repellent film ensures long life, extending lubrication intervals

- Thin film eliminates fling off and does not collect abrasive particles

- Ropes are clean to handle and allow easy inspection

- Extensive covering power, resulting in economic usage

Directions for Use

Apply sparingly (1kg is sufficient to lubricate up to 50m of 25mm dia rope). When the rope is in use, the capillary action of the lubricant will ensure full penetration to the core of the rope. Use straight from the container, even in cold weather. For best results, BIO-ROPELUBE 00 should be applied to clean ropes to ensure complete penetration.

Technical Data

Appearance	-	Grey-black semi-fluid grease

NLGI classification				-	00

Thickener					-	Bentone

Base fluid type	-	Vegetable oil

Viscosity of base oil @ 40ºC (IP71)	-	820 cSt

Solid lubricant	-	Molybdenum disulphide

Biodegradability (CEC-L-33-T-82)	-	>80%

Operating temperature range:	-	-30ºC to 120ºC

The content of this data sheet is given in good faith but without warranty.                     (June 20)